| PanTech | PANTECH TAPE CO. LTD. Tel: 886-3-475 8949 Fax : 886-3-475 8957 sales@pantechtape.com http://pantechtape.com/ | ® 3C |  |
| --- | --- | --- | --- |

No. 8, ALLEY 98, LANE 800, CHUNG-SHAN SOUTH ROAD, YANGMEI, TAOYUAN 32669, TAIWAN

### Cleaning Tape

PanTech Cleaning Tape, is specially designed for the cleaning process of the PCB (Printed Circuit Board) on the cleaning machine or web cleaning on the roll to roll converting process. It assures a proper adhesion to remove the unexpected material effectively from the PC board or processing web, with no adhesive residual after the cleaning process.

Characteristics：

| Catalog Number | PT - 683 | PT - 657 |
| --- | --- | --- |
| Peel Adhesion | 300 ~ 400 g./in. | 600 ~ 700 g./in. |
| Substrate | Plastic film | PET film |
| Film Thickness | 0.072 mm | 0.050 mm |
| Total Thickness | 0.084 mm | 0.073 mm |
| Tensile Strength | 18 Kg / in. | 16 Kg / in |
| Elongation | 120 % | 100 % |
| Adhesive | Solvent type Acrylic adhesive |
| Standard length | 20 M, 35 M, 40M |
| Width | Up to 1,500 mm |
| Color | White |
| Core | PE core, 3”, 6”, 1.5” |