| PanTech | PANTECH TAPE CO. LTD. Tel: 886-3-475 8949 Fax : 886-3-475 8957 sales@pantechtape.com http://pantechtape.com/ | ® 3C |  |
| --- | --- | --- | --- |

No. 8, ALLEY 98, LANE 800, CHUNG-SHAN SOUTH ROAD, YANGMEI, TAOYUAN 32669, TAIWAN

##### Permanent Sealing

##### BAG SEALING TAPE

|  | PanTech BAG SEALING TAPE is a permanent double side tape specially designed for hot knife automatic machine cuttable sealing of PE courier bags. The adhesive is strong enough to destroy the sealed plastic bags during opening. |
| --- | --- |

Characteristics：

| Cat. No. | PT – 15 |
| --- | --- |
| Release Liner | PEPA laminated with OPP |
| Width of release liner | 15 mm |
| Thickness of release liner | 0.08 mm |
| Carrier | PET film |
| Width of carrier | 14 mm |
| Thickness of carrier | 0.012 mm |
| Adhesive | Solvent type Acrylic adhesive |
| Adhesive Strength (Narrow Side) | 1,900 g / 8 mm |
| Adhesive Strength (Wide Side) | 400 g / 13.5 mm |
| Length | 500M, 5,000M (spool winding) |

# Text boxes

0.13mm

0.08mm PEPA/OPP

15 mm

0.012 mm PET

0.03mm

8 mm

13.5mm