| PanTech | PANTECH TAPE CO. LTD. Tel: 886-3-475 8949 Fax : 886-3-475 8957 sales@pantechtape.com http://pantechtape.com | ® 3C |
| --- | --- | --- |

NO. 8, ALLEY 98, LANE 800, CHUNG-SHAN SOUTH ROAD, YANGMEI, TAOYUAN, TAIWAN, R.O.C

PEN Electrical Tape

Silicone Adhesive, 180°C

PanTech PEN Electrical Tape is made of 1 mil Dupont® Kaladex PEN film coated with silicone adhesive. It performs an excellent thermal property, mechanical property and electrical property continuously in 180°C.  it also shows better dimensional stability, hydrolytic resistance and excellent oxygen permeability than that of PET film. It is a most suitable dielectric base film for the flexible printed circuitry (FPC) industry and F-class application in various kinds of electrical components industry. It provides an economic alternative for people who previously use the expensive polyimide film tape and polyamide paper laminates.

Characteristics:

| Catalog No. | 158 |
| --- | --- |
| Substrate | PEN (Polyethylene Naphthalene) film |
| Adhesive | Silicone |
| Temperature rating | 180℃ |
| Film thickness | 0.025 mm |
| Total thickness | 0.055 mm |
| Tensile strength | 10 kgs/in. |
| Elongation | 80 % |
| Breakdown voltage | 6 KV |
| Dielectric Strength | 1×1015Ω-cm (20℃) |
| Solvent resistance | excellent |
| Peel Adhesion | 800 g / in. |
| Length | 66 M |
| Color | Clear, white, yellow |