### POLYESTER ELECTRICAL TAPE

UL Recognized, 130℃,  E117836

|  | PanTech Polyester Electrical Insulating Tape has been UL recognized, 130℃, E117836. It has strong adhesion, outstanding tensile and dielectric strength, excellent heat and solvent resistance. It is most suitable for the wrapping and holding applications in transformers, capacitors, electric motors, relays, stabilizers and various kinds of electrical components. It is RoHS and REACH free. |
| --- | --- |

Characteristics:

| Catalog Number | PT-25 |
| --- | --- |
| Film Thickness | 0.025 mm |
| Total Thickness | 0.055 mm |
| Tensile Strength | 9.5 kg/in. |
| Elongation | 100 % |
| Dielectric Strength | DC 5KV, ac 3KV |
| Length | 50 M, 30M |
| Substrate | PET (Polyethylene Terephthalate) film |
| Specific Resistance | 1×1015Ω-cm (20℃) |
| Adhesive | Solvent type Acrylic adhesive |
| Temperature Rating | 130℃ |
| Solvent Resistance | excellent, |
| Peel Adhesion | > 600 g/in. |
| Standard width | 970 mm |
| Jumbo roll length | 1,500 M |
| Colors | yellow, red, blue, green, black, white and transparent. |