| PanTech | PANTECH TAPE CO. LTD. Tel: 886-3-475 8949 Fax : 886-3-475 8957 sales@pantechtape.com http://pantechtape.com | ® 3C | E117836 |
| --- | --- | --- | --- |

No. 8, ALLEY 98, LANE 800, CHUNG-SHAN SOUTH ROAD, YANGMEI, TAOYUAN 32669, TAIWAN

##### SPLICING TAPE

### FOR PHOTO PROCESSING

|  | PanTech PHOTO PROCESSING SPLICING TAPE is specially designed for splicing application in the photo processing procedure. It has a strong adhesion to the polyester photo film to ensure a solid splicing never to slip off during the photo processing procedure. It can resist the heat and processing chemicals. It can also be peeled with minimal residual on the photo film after the procedure. |
| --- | --- |

Characteristics：

| Cat. No. | PT – 256 | PT – 506 | PT-280 |
| --- | --- | --- | --- |
| Description | 1 mil, acrylic | 2 mil, acrylic | 2 mil, silicone |
| Film Thickness | 0.025 mm | 0.050 mm | 0.050 mm |
| Total Thickness | 0.055 mm | 0.080 mm | 0.080 mm |
| Tensile Strength | 9 kg/in. | 16 kg/in. | 16 kg/in. |
| Elongation | 100 % | 70 % | 70 % |
| Adhesive | Acrylic | Acrylic | Silicone |
| Colors | Yellow, black, clear | Yellow, black, clear | Light green |
| Substrate | PET film |
| Peel Adhesion to steel | 800 g/in |
| Peel Adhesion to PET | 800 g/in |
| Standard length | 66M, 50M |