| PanTech | PANTECH TAPE CO. LTD. Tel: 886-3-475 8949 Fax : 886-3-475 8957 sales@pantechtape.com http://pantechtape.com | ® 3C |
| --- | --- | --- |

NO. 8, ALLEY 98, LANE 800, CHUNG-SHAN SOUTH ROAD, YANGMEI, TAOYUAN, TAIWAN, R.O.C

Application Tapes

| PT - 40 OPP/acrylic/80°C |  | PT-41 PET/acrylic/140°C PT-43 PET/silicone/170°C |
| --- | --- | --- |
| OPP application tape for PVC cutting |  | Hot fix tape PET application tape |

| Cat. No. | Film | adhesive | Liner | Temp °C | Thick- ness,mm | Peel Ad. Kg / in. | Tensile kg / in. | Elonga- tion, % | Length M |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |

| PT40 | 40(OPP | acrylic | No | 80°C | 0.050 | 0.20 | 9.0 | 100 | 100 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| OPP Application tape, transfer and orientation of PVC cuttings |

| PT41 | 50(PET | acrylic | Release paper | 140°C | 0.090 | 1.10 | 9.5 | 100 | 100 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| PET Application tape, hot transfer/ironing fix onto clothes |

| PT43 | 50(PET | silicone | Embossed plastic | 170°C | 0.080 | 0.7 | 9.5 | 100 | 100 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Hot Fix Tape, PET/silicone, higher ironing temperature,170°C |