PanTech

PET APPLICATION TAPE

|  | PanTech PET Application tape, also called as hot fix tape or hot transfer tape, is specially designed for the transfer and orientation application of the plastic hologram patterns, artificial diamonds, or small articles onto clothes by iron or heat press. It assures not only a proper adhesion to remove the pattern articles from the release paper, also a clean removal after the transfer. It can be easily peeled off at a short time after the ironing. |
| --- | --- |

Characteristics:

| Catalog No. | 41 |
| --- | --- |
| Substrate | PET film |
| Peel Adhesion | 1,100 g/in. |
| Film Thickness | 0.050 mm |
| Adhesive | Solvent type Acrylic adhesive |
| Total thickness | 0.090 mm |
| Tensile Strength | 18 Kg / in |
| Elongation | 140 % |
| Standard Length | 100 M |
| Width | Up to 1,250 mm |
| Color | Transparent |