| PanTech | PANTECH TAPE CO. LTD. Tel: 886-3-475 8949 Fax : 886-3-475 8957 sales@pantechtape.com http://www.pantechtape.com | ® 3C |
| --- | --- | --- |

NO. 8, ALLEY 98, LANE 800, CHUNG-SHAN SOUTH ROAD, YANGMEI, TAOYUAN, 326,TAIWAN, R.O.C

### Hot Fix Tape,

### with silicone adhesive

|  | PanTech hot fix tape, also called as hot transfer tape or PET application tape, is specially designed for the transfer and orientation application of the plastic hologram patterns, artificial diamonds, or small articles onto clothes by iron or heat press. It assures not only a proper adhesion to remove the pattern articles from the release paper, also a clean removal after the transfer. It can be easily peeled off at a short time after the ironing. It can resist temperature up to 170 °C. |
| --- | --- |

Characteristics:

| Catalog No. | 43 |
| --- | --- |
| Substrate | 0.05 mm PET film |
| Peel Adhesion | 800 g/in. |
| Liner | Embossed plastic film |
| Adhesive | Silicone adhesive |
| Total thickness | 0.080 mm |
| Tensile Strength | 18 Kg / in |
| Elongation | 70 % |
| Standard Length | 100 M |
| Width | Up to 1,250 mm |
| Color | Transparent |